|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **TECHNOLOGY DATA SHEET Digital Printing paper** | | | |  |
| 100micron dtf paper for dtf printing | | | |  |
| This type is double side coated with cold and hot peel paper with excellent demensional stability | | | |  |
| DTF printing with water based pigment ink.Compare with the dtf film,paper is more eco friendly. | | | |  |
| Recycable and be friendly to environment. | | | |  |
| Property | Unit | Value |  |  |
| Thickness | μm | 105 |  |  |
| Weight | gsm | 100 |  |  |
| Release Force | g/inch | 7-10g |  |  |
| Transfer temperature | ℃ | 150 to 160 |  |  |
| Heat transfer Time | second | 5 to 8 |  |  |
|  |  |  |  |  |
| **Note:** Above mentioned data is reliable according to the latest state.However the user | | |  |  |
| need examine the stuitable film for individual application. | | |  |  |
|  |  |  |  |  |
|  |  |  |  |  |
|  |  |  |  |  |